07/16/2026

Include if project has concrete overlays for bridge decks.

## Section 569. — CONCRETE OVERLAYS FOR BRIDGE DECKS

Construction Requirements

569.04 Composition (Concrete Mix Design). Delete Table 569-1 and substitute the following:

Table 569-1

Composition of Concrete

| Concrete Overlay Class | Property |  |  |  |  | Performance Characteristics |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Total Cementitious Material Content, pounds per cubic yard(1) | Maximum Water/ Cementitious Material Ratio(4) | Slump, inches | Air Content, percent | Coarse Aggregate Size Number AASHTO M 43(5) | Minimum Apparent Surface Resistivity at 28 days, AASHTO T 358 (4 by 8 inch cylinder), kΩ.cm | Minimum Bond Strength at 14 days, ASTM C1583, pounds per square inch | Minimum Compressive Strength at 28 days, AASHTO T 22, pounds per square inch |
| HPC(O)(2) | 564 to 750 | 0.45 | 2 to 8 | Table 552-1 | 7, 78, 8 | 27 | 150 | 4500 |
| LMC(3) | 564 to 750 | 0.45 | 2 to 8 | 3.0 to 10.0 | 7, 78, 8 | 27 | 150 | 4000 |

(1) The total cementitious material content includes portland cement and pozzolans added to the concrete mixture (such as ground granulated blast furnace slag, fly ash, and silica fume). Meet the requirements shown in Table 552-2.

(2) Add 1.5 gallons per cubic yard of concrete of an approved Shrinkage Reducing Admixture (SRA).

(3) Add 3.5 gallons of latex emulsion admixture per 94 pounds of cement.

(4) Include the water contained in the aggregate above the amount of absorbed water in the calculation of the water-to-cementitious material ratio.

(5) Meet the processing requirements of AASHTO M 43, Table 1 – Standard Sizes of Processed Aggregate.

(6) AASHTO T 277 may be used instead of AASHTO T 358.  If using AASHTO T 277, convert test results to AASHTO T 358 results using S=5801.2(RCP)-0.819.

569.16 Concrete Curing. Delete the fifth paragraph and substitute the following:

Minimum apparent surface resistivity will be evaluated under Subsection 106.05. The specification limit is the shown in Table 569-1. A single surface resistivity test result is the average result from 3 samples cast from the same load and tested.

Only allow construction traffic for placement of bridge overlay on the bridge deck for the first 7 days of curing.

569.18 Acceptance.  Delete Table 569-2 and substitute the following:

Table 569-2

Sampling, Testing, and Acceptance Requirements

| Material or Product (Subsection) | Type of Acceptance (Subsection) | Characteristic | Category | Test Methods Specifications | Sampling Frequency | Point of Sampling | Split Sample | Reporting Time | Remarks |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Source |  |  |  |  |  |  |  |  |  |
| Aggregate (fine & coarse) | Measured & tested for conformance (106.04 & 105) | Quality | − | Subsections 703.01 & 703.02 | 1 per material type | Source of material | Yes, if requested | Before producing | Date reports within 1 year of intended use |
| Mix Design |  |  |  |  |  |  |  |  |  |
| Concrete composition | Measured & tested for conformance (106.04 & 105) | All | − | Subsection 569.04 | 1 per mix design | Source of material | Yes, if requested | Before producing | − |
| Production Start-up (Test Section) |  |  |  |  |  |  |  |  |  |
| HPC(O) | Measured & tested for conformance (106.04) | Minimum apparent surface resistivity(1) | − | AASHTO T 358 | 1 set per test placement | Discharge stream at point of placement (1) | Yes, if requested | Upon completing tests | − |
|  |  | Compressive strength(2) | − | AASHTO T 23 & 22 | " | " | " | " | − |
|  |  | Tensile bond strength | − | ASTM C1583 | 5 cores per test placement | In-place after curing is complete | " | " | − |
| LMC | Measured & tested for conformance (106.04) | Minimum apparent surface resistivity(1) | − | AASHTO T 358 | 1 set per test placement | Discharge stream at point of placement | Yes | Upon completing tests | − |
|  |  | Compressive strength(3) | − | AASHTO T 23 & 22 | " | " | " | " | − |
|  |  | Tensile bond strength(7) | − | ASTM C1583 | 5 cores per test placement | In-place after curing is complete | " | " | − |

Table 569-2 (continued)

Sampling, Testing, and Acceptance Requirements

| Material or Product (Subsection) | Type of Acceptance (Subsection) | Characteristic | Category | Test Methods Specifications | Sampling Frequency | Point of Sampling | Split Sample | Reporting Time | Remarks |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Production Start-up (Test Section) (continued) |  |  |  |  |  |  |  |  |  |
| HPC(O) and LMC | " | Density(4) | − | AASHTO T 121 | 1 per load | Point of discharge | No | Upon completing tests | − |
|  |  | Air content(4) | − | AASHTO T 152 or AASHTO T 196 | " | " | " | " | − |
|  |  | Slump(4),(5) | − | AASHTO T 119 | " | " | " | " | − |
|  |  | Temperature | − | Field measured | " | " | " | " | − |
| Aggregate (fine & coarse) | Measured & tested for conformance (106.04) | Gradation | − | AASHTO T 27 & T 11 | 1 per day | Flowing aggregate stream (bin, belt, discharge conveyor belt, or stockpile) | Yes | Before batching | − |
|  |  | Fineness modulus | − | AASHTO T 27 | − | " | " | " | − |
|  |  | Moisture test | − | AASHTO T 255 | − | " | " | " | − |
| Production |  |  |  |  |  |  |  |  |  |
| HPC(O) & LMC | Statistical (106.05) | Minimum apparent surface resistivity(1) | II | AASHTO T 277 | 1 set per 30 yd3 but not less than 1 per day | Discharge stream at point of placement | Yes | Upon completing tests | − |
|  |  | Compressive strength(6) | II | AASHTO T 23 & T 22 | " | " | " | " | − |
|  |  | Tensile bond strength(7) | II | ASTM C1583 | 1 set per 3000 ft2 of overlay but not less than 1 per day | In-place after curing is complete | No | " | − |

Table 569-2 (continued)

Sampling, Testing, and Acceptance Requirements

| Material or Product (Subsection) | Type of Acceptance (Subsection) | Characteristic | Category | Test Methods Specifications | Sampling Frequency | Point of Sampling | Split Sample | Reporting Time | Remarks |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Production (continued) |  |  |  |  |  |  |  |  |  |
| HPC(O) & LMC | Measured & tested for conformance (106.04) | Density(4) | − | AASHTO T 121 | 1 per load | Point of discharge | No | Upon completing tests | − |
|  |  | Air content(4) | − | AASHTO T 152 or AASHTO T 196 | " | " | No | " | − |
|  |  | Slump(4),(5) | − | AASHTO T 119 | " | " | " | " | − |
|  |  | Temperature | − | ASTM C1064 | " | " | " | " | − |
| Aggregate (fine & coarse) | Measured & tested for conformance (106.04) | Gradation | − | AASHTO T 27 & T 11 | 1 per day | Flowing aggregate stream (bin, belt, discharge conveyor belt, or stockpile) | Yes, if requested | Before batching | − |
|  |  | Fineness modulus | − | AASHTO T 27 | − | " | " | " | − |
|  |  | Moisture test | − | AASHTO T 255 | − | " | " | " | − |

Table 569-2 (continued)

Sampling, Testing, and Acceptance Requirements

(1) Cast at least three 4- by 8-inch minimum apparent surface resistivity cylinders per set and carefully transport the cylinders to the job site curing facility. Cure the HPC(O) cylinders according to AASHTO M 201. Test for surface resistivity at 28 days according to AASHTO T 358. The test result is the average of the measurements on three cylinders cast from the same load. If pigment is used in the concrete mixture, sample concrete at the batch plant before and after adding pigment. Test at least three specimens with and without pigment. Determine the average difference between the pigmented and non-pigmented test results. Adjust production test results by the average difference. Report both initial and adjusted test results. After completion of resistivity testing, at 28 days the same cylinders may be used for compressive strength testing. (2) For HPC(O), cast at least fifteen 4- by 8-inch compressive strength cylinders per set and carefully transport the cylinders to the job site curing facility. Test three cylinders each at 1, 3, 7, 14 and 28 days. A single compressive strength test result is the average result from three cylinders cast from the same load. (3) For LMC, cast at least eighteen 4- by 8-inch compressive strength cylinders per set and carefully transport the cylinders to the job site curing facility. Test three cylinders each at 1, 2, 4, 7, 14 and 28 days. A single compressive strength test result is the average result from three cylinders cast from the same load. (4) For LMC, measure density, slump, and plastic air content 5 minutes after discharge from the mixer chute. Cover wheelbarrow or other receptacle used to hold sample with a sheet of plastic to prevent evaporation during the 5 minutes before sampling. (5) If reinforcing fibers are used at an addition rate greater than 0.3 percent by volume, measure slump at the batch plant before adding fibers. (6) Cast at least six 4- by 8-inch compressive strength cylinders per set and carefully transport the cylinders to the job site curing facility. Test three cylinders at 28 days. Use the remainder of cylinders as directed. (7) At random locations determined by the CO, core 2-inch diameter specimens through the overlay and ½ inch into the substrate concrete. Cure the specimens in situ for the same length of time as the overlay. Test the specimens in situ by attaching a loading disk with fast setting, high strength epoxy. Measure the tensile pull-off bond strength in pounds per square inch according to ASTM C1583. The average bond strength is the average of the results from three test specimens adjusted as follows: For tests where failure occurs in the substrate concrete at a depth of at least ¼ inch for more than 50 percent of the specimen, use 150 pounds per square inch for that specimen test result in the calculation of the average of the three test specimens. When two of the three test results have been adjusted, the average bond strength results use the greater of 150 pounds per square inch or the calculated value.