04/21/2025

## Section 610. — SIDEWALKS, PADS, AND MEDIANS

Include if project has concrete curb or concrete curb and gutter.

**Material**

**610.02** Add the following:

Curing material 711.01

**Construction Requirements**

**610.04 Concrete Sidewalks, Pads, and Medians.** Delete the last paragraph, and substitute the following:

Use a ¼-inch radius edging tool on slab edges and joints. Cure concrete at least 7 days. Use a liquid membrane forming compound for curing. Use Type 1-D, clear liquid membrane forming compound on colored concrete. Use Type 2, white pigmented liquid membrane forming compound on non-colored concrete.

Immediately after applying the liquid membrane forming compound, cover the concrete with waterproof sheet material to prevent moisture loss from the concrete. Use the widest sheets practical. Lap adjacent sheets at least 12 inches and tightly seal seams with pressure sensitive tape, mastic, glue, or other approved methods. Secure material so that wind does not displace it. Immediately repair sheets that are broken or damaged. Keep the concrete covered for the curing period.

Remove and replace cracking, spalling, or scaling concrete to the nearest joint.