INCLUDE SECTION 407 ON ALL PROJECTS WITH CHIP SEAL

$$407.00A

Section 407. — CHIP SEAL

Revised 07 April 2026

INCLUDE THE FOLLOWING ON ALL PROJECTS WITH CHIP SEAL

$$407.11A

407.11.  Delete the second sentence of the first paragraph and substitute the following:

Table 407-1 application rates are for estimating purposes only.

INCLUDE THE FOLLOWING ON ALL PROJECTS WITH CHIP SEAL

##407.13A

Delete Table 704-3 and substitute the following:

Table 407-3

Sampling, Testing, and Acceptance Requirements

| Material or Product (Subsection) | Type of Acceptance (Subsection)(3) | Characteristic | Category | Test Methods Specifications | Sampling Frequency | Point of Sampling | Split Sample | Reporting Time | Remarks |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Source |  |  |  |  |  |  |  |  |  |
| Chip seal aggregate(1) (703.09) | Measured & tested for conformance (106.04 & 105) | Quality | − | Subsection 703.09 | 1 per material type | Source of material | Yes | Before producing | − |
|  | Process control (153.03) | Gradation | − | AASHTO T 27 & T 11 | 2 per day per stockpile | Crusher belt (during production) | No | 24 hours | Not required if using a pre-crushed commercial source |
| Blotter (703.12) | " | " | − | Subsection 703.12 | " | " | " | " | − |
| Asphalt binder(2) (702.01) or emulsified asphalt(2) (702.02) | Measured & tested for conformance (106.04) | Quality | − | Section 702 | 1 per material type | Point of shipment or delivery | Yes(4) | Before incorporating into work | − |

Table 407-3 (continued)

Sampling, Testing, and Acceptance Requirements

| Material or Product (Subsection) | Type of Acceptance (Subsection)(3) | Characteristic | Category | Test Methods Specifications | Sampling Frequency | Point of Sampling | Split Sample | Reporting Time | Remarks |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Production |  |  |  |  |  |  |  |  |  |
| Chip seal aggregate(1) (703.09) | Statistical(3) (106.05) | Gradation (See Table 703-5 for applicable sieves) | I | AASHTO T 27 & T 11 | (3) | Spreader discharge | Yes | 24 hours | − |
|  | Process control (153.03) | Moisture on surface of aggregates | − | Visual inspection (407.10) | Contractor determined | Stockpile or spreader discharge | No | Before incorporating into work | − |
| Asphalt binder(2) (702.01) or emulsified asphalt(2) (702.02) | Measured & tested for conformance (106.04) | Quality | − | Section 702 | 1 per tanker truck including trailer | Tanker or Distributor | Yes(4) | − | Tested by Government |
|  | Process control (153.03) | Placement temperature | − | − | 1 per distributor truck minimum | Distributor truck | No | Before incorporating into work | − |

(1) Applies to each aggregate grade provided.

(2) Applies to each asphalt material provided.

(3) For plan quantities less than 40,000 square yards, material will be accepted according to Subsection 106.03. For plan quantities equal to or greater than 40,000 square yards, material will be accepted according to Subsection 106.05. For plan quantities between 40,000 and 240,000 square yards, the sampling frequency will be determined by dividing the plan quantity by eight. If plan quantity exceeds 240,000 square yards, the sampling frequency will be one every 30,000 square yards.

(4) Two 1-quart samples for asphalt binder. One 1-gallon sample for emulsified asphalt.