[bookmark: _Hlk227853558]INCLUDE SECTION 407 ON ALL PROJECTS WITH CHIP SEAL
$$407.00A
Section 407. — CHIP SEAL
Revised 07 April 2026

INCLUDE THE FOLLOWING ON ALL PROJECTS WITH CHIP SEAL
$$407.11A
407.11.  Delete the second sentence of the first paragraph and substitute the following:

Table 407-1 application rates are for estimating purposes only.







INCLUDE THE FOLLOWING ON ALL PROJECTS WITH CHIP SEAL
##407.13A
Delete Table 704-3 and substitute the following:

Table 407-3
Sampling, Testing, and Acceptance Requirements
	Material or
Product
(Subsection)
	Type of
Acceptance
(Subsection)(3)
	Characteristic
	Category
	Test Methods
Specifications
	Sampling
Frequency
	Point of
Sampling
	Split
Sample
	Reporting
Time
	Remarks

	Source

	Chip seal
aggregate(1) (703.09)
	Measured & tested for conformance
(106.04 & 105)
	Quality
	−
	Subsection
703.09
	1 per
material type
	Source of
material
	Yes
	Before
producing
	−

	
	Process
control
(153.03)
	Gradation
	−
	AASHTO
T 27 & T 11
	2 per day per stockpile
	Crusher belt
(during
production)
	No
	24 hours
	Not required if using a pre-crushed commercial source

	Blotter
(703.12)
	"
	"
	−
	Subsection
703.12
	"
	"
	"
	"
	−

	Asphalt binder(2) (702.01) or emulsified asphalt(2) (702.02)
	Measured &
tested for
conformance
(106.04)
	Quality
	−
	Section
702
	1 per
material type
	Point of
shipment
or
delivery
	Yes(4)
	Before
incorporating
into work
	−



Table 407-3 (continued)
Sampling, Testing, and Acceptance Requirements
	Material or
Product
(Subsection)
	Type of
Acceptance
(Subsection)(3)
	Characteristic
	Category
	Test Methods
Specifications
	Sampling
Frequency
	Point of
Sampling
	Split
Sample
	Reporting
Time
	Remarks

	Production

	Chip seal
aggregate(1) (703.09)
	Statistical(3)
(106.05)
	Gradation
(See Table
703-5 for
applicable
sieves)
	I
	AASHTO
T 27 & T 11
	(3)
	Spreader
discharge
	Yes
	24 hours
	−

	
	Process control
(153.03)
	Moisture on
surface of
aggregates
	−
	Visual
inspection
(407.10)
	Contractor
determined
	Stockpile
or spreader
discharge
	No
	Before
incorporating
into work
	−

	Asphalt
binder(2) (702.01)
or
emulsified
asphalt(2) (702.02)
	Measured &
tested for
conformance
(106.04)
	Quality
	−
	Section
702
	1 per
tanker truck
including
trailer
	Tanker
or
Distributor
	Yes(4)
	−
	Tested by
Government

	
	Process control
(153.03)
	Placement
temperature
	−
	−
	1 per
distributor
truck minimum
	Distributor
truck
	No
	Before
incorporating
into work
	−


(1) Applies to each aggregate grade provided.
(2) Applies to each asphalt material provided.
[bookmark: _Hlk225754733](3) For plan quantities less than 40,000 square yards, material will be accepted according to Subsection 106.03. For plan quantities equal to or greater than 40,000 square yards, material will be accepted according to Subsection 106.05. For plan quantities between 40,000 and 240,000 square yards, the sampling frequency will be determined by dividing the plan quantity by eight. If plan quantity exceeds 240,000 square yards, the sampling frequency will be one every 30,000 square yards.
(4) Two 1-quart samples for asphalt binder. One 1-gallon sample for emulsified asphalt.  

