INCLUDE SECTION 501 ON ALL PROJECTS WITH CONCRETE PAVEMENT (THIS INCLUDES PROJECTS WITH EITHER 501 OR 502 PAY ITEMS)

$$501.00A

Section 501. — MINOR CONCRETE PAVEMENT

Revised 15 December 2025

INCLUDE CLAUSES ##501.03A AND ##501.03B ON ALL PROJECTS WITH CONCRETE PAVEMENT

##501.03A

501.03.  Delete the second sentence and substitute the following:

Submit concrete mix designs for approval on Form FHWA1606, Minor Portland Cement Concrete Mix Design, at least 30 days before production.

##501.03B

501.03.  Delete Table 501-1 and substitute the following:

Table 501-1

Composition of Concrete

| Maximum Water/ Cementitious Material Ratio | Maximum Slump AASHTO T 119, inch | Minimum Air Content, percent | Maximum Coarse Aggregate Size AASHTO M 43, Inch(1) | Minimum 28-Day Compressive Strength AASHTO T 22, pounds per square inch |
| --- | --- | --- | --- | --- |
| 0.45 | 4 (fixed form) | 5.0 | 1½ | 4000 |

(1) Meet size number gradation and requirements from AASHTO M 43 for coarse aggregates. Blending of standard sizes to optimize gradation is allowed.