## Section 565. — drilled shafts

01 APR 2024 – FP-24

WFL Specification 01 APR 2024

Include the following when Drilled Shafts are required.

### 565.08 Concrete for Drilled Shafts..

Delete Table 565-4 and substitute the following:

Table 565-4

Concrete for Drilled Shafts

|  |  |  |  |
| --- | --- | --- | --- |
| Method | Class | Slump | Coarse Aggregate Size Number(2) |
| Shafts constructed without drilling fluid | A(1) | 7±1 inches | 8, 89 |
| Shafts constructed with drilling fluid | A(1) | 8±1 inches | 8, 89 |
| Shafts for underwater placement | S | – | 5, 56, 57 |

(1) Use Class A(AE) concrete on portions of the drilled shaft above the finished ground-line unless otherwise noted.

(2) Meet the processing requirements of AASHTO M 43, *Table 1 – Standard Sizes of Processed Aggregate*.