US DEPARTMENT OF TRANSPORTATION – FEDERAL HIGHWAY ADMINISTRATION

Construction Inspection Checklist

Section 309 Emulsified Asphalt-Treated Base Course

| Project Name: | Project No.: |
| --- | --- |
| Date: | Weather: |
| Contractor: | Subcontractor: |
| Inspector: | Location/Station: |
| Description of work being inspected: |  |

| Conformance | CHECKS (characteristics) |  |
| --- | --- | --- |
| Yes No N.A. |  |  |
|  | General |  |
|  | 1. Was the surface on which the treated aggregate base course was placed, prepared according to section 204 or 303 as applicable? (309.03) |  |
|  | 2. After a representative quantity of aggregate was produced, were proposed target values submitted for the appropriate sieve sizes along with a representative 300-pound sample at least 14 days before incorporating the aggregate into the work? (309.03) |  |
|  | 3. Were target values set within the gradation ranges shown in table 703-2 for the required grading? (309.03) |  |
|  | Mixing and Spreading |  |
|  | 4. Was a stationary pugmill with weighing, volumetric or other gauging equipment capable of accurately controlling the material entering the mixer used? (309.04) |  |
|  | 5. Were the controls for the aggregate feed with the emulsified asphalt and water controls interlocked to ensure uniform introduction of material into the mixer? (309.04) |  |
|  | 6. Was the optimum moisture content determined according to AASHTO T 180, Method D? (309.04) |  |
|  | 7. Was the material mixed in the following sequence: (1) Add the aggregate and water to the mixer before the emulsified asphalt, (2) Add 1 percent emulsified asphalt by mass of aggregate, (3) Adjust the total liquid content (emulsified asphalt and water) so that, at the time of compaction, the total content is within 2 percent of the optimum moisture content, and (4) Mix until all particles are uniformly coated? (309.04) |  |
|  | 8. Immediately after mixing, was the mixture spread on the prepared surface in a uniform layer? (309.04) |  |
|  | 9. Was the mixture shaped to line, grade and cross-section? (309.04) |  |
|  | 10. Was hauling equipment routed uniformly over the full width of the surface to minimize rutting or uneven compaction? (309.04) |  |
| Conformance | CHECKS (characteristics) |  |
| Yes No N.A. |  |  |
|  | Compacting |  |
|  | 11. Was maximum density of the mixture determined by AASHTO T 180, method D? (309.05) |  |
|  | 12. Was the mixture compacted full width, rolled from the sides to the center, parallel to the centerline? (309.05) |  |
|  | 13. Was the mixture along curbs, headers, walls, and all places not accessible to the roller compacted with an approved tamper or compactor? (309.05) |  |
|  | 14. Was the mixture compacted to at least 95 percent of maximum density? (309.05) |  |
|  | 15. Was the in place density and moisture content determined according to AASHTO T 310. (309.05) |  |
|  | Surface Tolerance |  |
|  | 16. Was the surface finished according to subsection 301.06? (309.06) |  |
|  | Maintenance |  |
|  | 17. Was the treated aggregate course maintained to the correct line, grade, and cross-section until placement of the next course? (309.07) |  |
|  | 18. Were all defects corrected according to Subsection 301.06? (309.07) |  |
|  | 14. |  |
|  | 15. |  |
|  | 16. |  |
| Percent Conformance Calculations |  | YesYes + No(100)= (100)= % Conformance |

Comments: